浮选机技术参数                                  表1

| XJZ、JJF型自吸气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating flotation machine with auto air suction |  |  |  |  |  |  |  |  |
| JJF型浮选机搅拌程度适中，固体颗粒悬浮良好，不沉槽，停车不用放矿；液面平稳，分选效率高；叶轮浸没深度浅，圆周速度低，功耗省；易损件寿命长，维修方便；没有假底和异流管理；具有自吸空气能力。 |  |  |  |  |  |  |  |  |
| SF与JJF型浮选机机组。该机组利用SF型浮选机有自吸矿浆能力而作吸入槽，JJF型浮选机作直流槽，整个机组可水平配置，不用泡沫泵。 |  |  |  |  |  |  |  |  |
| Model JJF has a moderate agitating strength, the solid particles being well suspended without settlement and no need for cleaning-up when stopped. The liquid surface is kept stable and it has higher flotation recovery. Due to the impeller has a shallow immerging depth and low periphery speed, it consumes less power and its wearable parst have longer service life featuring easy maintenance. Dummy bottom and honeycomb duct are furnisher. This machine has auto aeration ability. |  |  |  |  |  |  |  |  |
| Flotation set of models SF and JJF works in a manner that model SF is taken as the suction function cell utilizing its auto suction ability, while model JJF works as a direct flow cell. Whole set may be installed horizontal and needs no foam pump. |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-1 |
|  | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机 功率 | 空气吸入量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| XJZ-3.5 | 0.35 | 700×700×700 | 300/160 | 470/787 | 0.18/0.4 | 2.2/0.55 | 0.9-1 | 450 |
| XJZ-6.2 | 0.62 | 900×900×850 | 350/216 | 400/583 | 0.3-0.9 | 4/1.1 | 0.9-1 | 870 |
| XJZ-11 | 1.1 | 1100×1100×1000 | 500/280 | 330/485 | 0.6-1.6 | 5.5/1.1 | 0.9-1.1 | 1500 |
| XJZ-28 | 2.8 | 1750×1600×1100 | 600/350 | 280/360 | 1.5-3 | 11/1.1 | 0.9-1 | 2200 |
| XJZ-58 | 5.8 | 2200×2200×1200 | 750/430 | 240/320 | 3--6 | 17/1.5 | 0.9-1 | 3900 |
| JJF-1 | 1 | 1400×1400×650 | 280 | 443 | 0.3-1 | 5.5/1.1 | 1 |  |
| JJF-2 | 2 | 1400×1400×1150 | 280 | 443 | 0.5-2 | 5.5/1.1 | 1 |  |
| JJF-3 | 3 | 1500×1850×1200 | 350 | 360 | 1-3 | 11/1.5 | 1 |  |
| JJF-4 | 4 | 1600×2150×1250 | 410 | 305 | 2-6 | 11/1.5 | 1 | 2302 |

表2

| XJZ、JJF型自吸气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating flotation machine with auto air suction |  |  |  |  |  |  |  |  |
| JJF型浮选机搅拌程度适中，固体颗粒悬浮良好，不沉槽，停车不用放矿；液面平稳，分选效率高；叶轮浸没深度浅，圆周速度低，功耗省；易损件寿命长，维修方便；没有假底和异流管理；具有自吸空气能力。 |  |  |  |  |  |  |  |  |
| SF与JJF型浮选机机组。该机组利用SF型浮选机有自吸矿浆能力而作吸入槽，JJF型浮选机作直流槽，整个机组可水平配置，不用泡沫泵。 |  |  |  |  |  |  |  |  |
| Model JJF has a moderate agitating strength, the solid particles being well suspended without settlement and no need for cleaning-up when stopped. The liquid surface is kept stable and it has higher flotation recovery. Due to the impeller has a shallow immerging depth and low periphery speed, it consumes less power and its wearable parst have longer service life featuring easy maintenance. Dummy bottom and honeycomb duct are furnisher. This machine has auto aeration ability. |  |  |  |  |  |  |  |  |
| Flotation set of models SF and JJF works in a manner that model SF is taken as the suction function cell utilizing its auto suction ability, while model JJF works as a direct flow cell. Whole set may be installed horizontal and needs no foam pump. |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-2 |
| 型号 规格 | 容积 | 槽体尺寸 | 叶轮 直径 | 叶轮 转速 | 处理 能力 | 电机 功率 | 空气 吸入量 | 单槽 质量 |
| Model | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| JJF-5 | 5 | 1600×2150×1550 | 410 | 305 | 2-6 | 11/1.5 | 1 | 2416 |
| JJF-8 | 8 | 2200×2900×1400 | 540 | 233 | 4-10 | 22/1.5 | 1 | 4500 |
| JJF-10 | 10 | 2200×2900×1700 | 540 | 233 | 4-12 | 22/1.5 | 1 | 4820 |
| JJF-16 | 16 | 2850×3800×1700 | 700 | 180 | 5-16 | 37/1.5 | 1 | 8000 |
| JJF-20 | 20 | 2850×3800×2000 | 700 | 180 | 2-20 | 37/1.5 | 1 | 8500 |
| JJF-24 | 24 | 3150×4150×2000 | Ф |  | 7-24 | 45 | 1 | 9180 |
| JJF-28 | 28 | 3150×4150×2300 | Ф |  | 7-28 | 55 | 1 | 9800 |
| JJF-42 | 42 | 3600×4800×2650 | Ф |  | 12-42 | 75 | 1 | 21000 |
| JJF-4Ⅱ | 4 | 1600×2150×1250 | 410 | 305 | 2-6 | 11/1.5 | 1 | 2302 |
| JJF-8Ⅱ | 8 | 2200×2900×1400 | 540 | 233 | 4-10 | 22/1.5 | 1 | 4500 |
| JJF-10Ⅱ | 10 | 2200×2900×1700 | 540 | 233 | 4-12 | 22/1.5 | 1 | 4820 |
| JJF-16Ⅱ | 16 | 2850×3800×1700 | 700 | 180 | 5-16 | 37/1.5 | 1 | 8000 |
| JJF-20Ⅱ | 20 | 2850×3800×2000 | 700 | 180 | 5-20 | 37/1.5 | 1 | 8500 |
| JJF-24Ⅱ | 24 | 3150×4150×2000 |  |  | 7-24 | 45 | 1 | 9180 |
| JJF-28Ⅱ | 28 | 3150×4150×2300 |  |  | 7-28 | 55 | 1 | 9800 |
| JJF-42Ⅱ | 42 | 3600×4800×2650 |  |  | 12-42 | 75 | 1 | 21000 |

表3

| XJ、XJQ、SF型自吸气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating flotation machine with auto air suction |  |  |  |  |  |  |  |  |
| SF型浮选机采用了结构新颖的前倾式槽体,双叶片水轮,配有导流管和假底装置,槽内矿浆按固定的流动方式进行上、下双循环，有利于粗粒矿物的悬浮，可自吸空气，自吸矿浆，不需泡沫泵。 |  |  |  |  |  |  |  |  |
| New siructure of impeller is backwards inclined double impellers equipped with honeyconb duct and dummy bottom.Therefore,the slurry in the tand will cycle upward and downward in a fixed flow manner,which is helpful to the suspension of those coarse particles.Airand slurry are naturally sucked without need for foam pump. |  |  |  |  |  |  |  |  |
| XJQ型浮选机为仿维姆科型，该机主要有以下几个特点：（1）采用了假底，循环简可使循环量达到槽容积的2.5倍;(2)定子结构为圆筒型,内壁设有立筋条和长孔,对矿浆的前切作用好;(3)转子浸没深度浅,叶轮转速低,叶轮和定子间隙大,所以其磨损轻,动力消耗大大减少;(4)可自吸空气。 |  |  |  |  |  |  |  |  |
| Model XJQ has following features：（1）Dummy bottom is adopted,making the recycling capacity of the recycling cylinder is 2.5times of the tand.(2)The stator is a cylinder in structure with its inner wall being vertically ribbed,and slots are placed,leading to better cutting lffect to the slurry.(3)Due to low immerging depth of the rotator,low rurning speed of the impeller,and wide space between the impeller and stator,wearing is low and power consumption greatly reduced.(4)It is spontaneously aerated. |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-3 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机功率 | 空气 吸入量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| XJ-1 | 0.13 | 500×500×550 | 200 | 593 | 0.05-0.16 | 1.5/0.55 | 0.25 | 318 |
| XJ-2 | 0.23 | 600×600×650 | 250 | 504 | 0.12-0.28 | 3/0.55 | 0.35 | 364 |
| XJ-3 | 0.35 | 700×700×700 | 300 | 483 | 0.18-0.4 | 2.2/0.55 | 0.5 | 430 |
| XJ-6 | 0.62 | 820×900×850 | 350 | 400 | 0.3-0.9 | 3/1.1 | 1 | 755 |
| XJ-11 | 1.1 | 1100×1100×1000 | 500 | 330 | 0.6-1.6 | 5.5/1.1 | 1.1 | 1416 |
| XJ-28 | 2.8 | 1750×1600×1100 | 600 | 280 | 1.5-3.5 | 11/1.1 | 2.5 | 2113 |
| XJ-58 | 5.8 | 2200×2200×1200 | 750 | 240 | 3--7 | 22/1.5 | 4 | 3400 |
| XJQ-20 | 20 | L×B×H | 320 | 352 | 1-2.5 | 7.5/1.1 | 0.1-1 |  |
| XJQ-40 | 4 | 1600×2100×1350 | 400 | 290/315 | 2--5 | 11/1.5 | 0.1-1 | 3075 |
| XJQ-80 | 8 | 2200×3000×1400 | 560 | 205/225 | 4--10 | 22/1.1 | 0.1-1 | 4585 |
| XJQ-100 | 10 | L×B×H | 540 | 233 | 6--10 | 22/1.5 | 0.1-1 | Q |

表4

| XJ、XJQ、SF型自吸气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating flotation machine with auto air suction |  |  |  |  |  |  |  |  |
| SF型浮选机采用了结构新颖的前倾式槽体,双叶片水轮,配有导流管和假底装置,槽内矿浆按固定的流动方式进行上、下双循环，有利于粗粒矿物的悬浮，可自吸空气，自吸矿浆，不需泡沫泵。 |  |  |  |  |  |  |  |  |
| New siructure of impeller is backwards inclined double impellers equipped with honeyconb duct and dummy bottom.Therefore,the slurry in the tand will cycle upward and downward in a fixed flow manner,which is helpful to the suspension of those coarse particles.Airand slurry are naturally sucked without need for foam pump. |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-4 |
| 型号规格 | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机功率 | 空气吸入量 | 单槽质量 |
| Model | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| XJQ-160 | 16 | 2800×3800×1700 | 700 | 170/180 | 8--20 | 30/1.5 | 0.1-1 | 8351 |
| XJQ-200 | 20 | L×B×H | 700 |  | 8--20 | 37/1.5 | 0.1-1 | Q |
| XJQ-280 | 28 | 3000×4150×2400 | 760 | 166/185 | 14-35 | 55/1.5 | 0.1-1 | Q |
| SF-0.15 | 0.15 | 500×500×600 | 200 | 536 | 0.06-0.18 | 1.5/0.55 | 0.8-1 | 269 |
| SF-0.37 | 0.37 | 700×700×750 | 296 | 386 | 0.2-0.4 | 1.5/0.55 | 0.8-1 | 468 |
| SF-0.7 | 0.7 | 820×900×950 | 350 | 400 | 0.3-0.9 | 3/1.1 | 0.8-1 | 805 |
| SF-1.2 | 1.2 | 1100×1100×1100 | 450 | 312 | 0.6-1.2 | 5.5/1.1 | 1-1.2 | 1373 |
| SF-2.8 | 2.8 | 1700×1600×1150 | 550 | 268 | 1.5-3.5 | 11/1.5 | 1-1.2 | 2138 |
| SF-4 | 4 | 1850×2050×1200 | 650 | 220 | 2--4 | 15/1.5 | 1-1.2 | 2582 |
| SF-8 | 8 | 2200×2900×1400 | 760 | 191 | 4--8 | 30/1.5 | 0.9-1 | 4129 |
| SF-10 | 10 | 2200×2900×1700 | 760 | 191 | 5--10 | 30/1.5 | 0.9-1 | 4486 |
| SF-16 | 16 | 2850×3800×1700 | 760 | 191 | 5--16 | 30×2/1.5 | 0.9-1 | 8320 |
| SF-20 | 20 | 2850×3800×2000 | 760 | 191 | 5--20 | 30×2/1.5 | 0.9-1 | 9828 |
| SF/JJF型自吸气机械搅拌式浮选机组技术参数 |  |  |  |  |  |  |  |  |
| specification of mechanical agitating flotation machine with auto air suction |  |  |  |  |  |  |  |  |
| SF/JJF-3 | 3 | 1700×1600×1150 | 550/350 | 268/360 | 1-3 | 11/1.5 | 1-1.2 |  |
| SF/JJF-4 | 4 | 1850×2050×1200 | 650/410 | 220/305 | 2-4 | 15/11/1.5 | 0.9-1 | 2582/2302 |
| SF/JJF-8 | 8 | 2200×2900×1700 | 760/540 | 191/233 | 4-8 | 30/22/1.5 | 0.9-1 | 4129/4500 |
| SF/JJF-16 | 16 | 2850×3800×1700 | 760/700 | 191/180 | 5-16 | 30/37/1.5 | 0.9-1 | 8320/8000 |
| SF/JJF-20 | 20 | 2850×3800×2000 | 760/700 | 191/180 | 5-20 | 30/37/1.5 | 0.9-1 | 9828/8500 |

表5

| BF、XJB型自吸气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating flotation machine with auto air suction |  |  |  |  |  |  |  |  |
| BF型浮选机叶轮是由闭式双截锥体组成，可产生强的矿浆下循环，其特点：（1）、吸气量大，功耗低。（2）、每槽兼有吸气、吸浆和浮选三重功能，自成浮选回路，不需任何辅助设备，水平配置，便于流程变更。（3）矿浆循环合理，能最大限度地减少粗砂沉淀。（4）设有矿浆面的自控和电控装置，调节方便。 |  |  |  |  |  |  |  |  |
| Impeller of model BF floation cell is composed of the dosed double section cones and ot can produce strong slutty cycle doumward.Its features are as follows:(1)The capacity of air suction is large,the power consumption is low.(2)Every tand has three functions of air suction,slurry suction and floation simultaneously being unique in floation return circuit without need for any supplementary equipment,the circuit change is convenient for horizontal location.(3)The slurry cycle is rational,the settlement of coarse sand can be reduced into full play.(4)The regulation is convenient to equip auto and electro-controlling arrangements for slutty level. |  |  |  |  |  |  |  |  |
| XJB型浮选机由斜棒轮、凸台、弧型稳流板构成充气搅拌器组，其特点有：（1）斜棒轮由铸铁铸造合在一起的圆盘和12根锥型棒条构成，可以衬胶，使用寿命长。（2）棒条与棒轮相反方向后倾45°角，且自上而下向外扩张15°锥角，搅拌强烈，防止槽底沉砂。（3）棒轮深度浅，停车后易于启动，有利于提高充气量，节省能耗。（4）可自吸浆，自吸空气，无需泡沫泵。 |  |  |  |  |  |  |  |  |
| Model XJB floation cell forms enforced aeration agitating machine set of skew wheel,boss and creeent regulating arc. Its features are as follows;(1)Skew bar wheel is composed of disk and 11pieces of cone-bar strip cast together in casting iron, and it can be lined with gum to prolong the service life.(2)Bar strip and bar wheel bend backward 45 in the opposite direetion and extent outward a cone apex apex angle with 15 from top to bottom, therefore its agitation is strong, the settlement of sand on the bottom of tank can be protected.(3)Due to low immerging depth of the bar wheel, the staring is easy during stopped condition and this is advantageous to incresaing the aeration capacity and saving on energy consumption.(4) It is able to suck slurry and air automatically without foam pump. |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-5 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮周速 | 处理能力 | 电机 功率 | 空气吸入量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | mm | mm | m/s | m3/min | kw | m3/m2min | kg |
| BF-0.15 | 0.15 | 550×550×600 | 200 | 6 | 0.06-0.16 | 2.2/0.55 | 0.9-1.05 | 270 |
| BF-0.25 | 0.25 | 650×600×700 | 250 | 6 | 0.12-0.28 | 1.5/0.55 | 0.9-1.05 | 370 |

表6

| BF、XJB型自吸气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating flotation machine with auto air suction |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-6 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮周速 | 处理能力 | 电机 功率 | 空气吸入量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | mm | mm | m/s | m3/min | kw | m3/m2min | kg |
| BF-0.37 | 0.37 | 740×740×750 | 286 | 7.2 | 0.2-0.4 | 1.5/1.1 | 0.9-1.05 | 470 |
| BF-0.65 | 0.65 | 850×950×900 | 300 | 7.35 | 0.3-0.7 | 3/1.1 | 0.9-1.1 | 932 |
| BF-1.2 | 1.2 | 1050×1150×1100 | 450 | 7.02 | 0.6-1.2 | 5.5/1.1 | 0.9-1.1 | 1370 |
| BF-2.0 | 2 | 1400×1450×1120 | 500 | 7.5 | 1--2 | 7.5/1.1 | 0.9-1.1 | 1750 |
| BF-2.8 | 2.8 | 1650×1650×1150 | 550 | 8.06 | 1.4-3 | 11/1.5 | 0.9-1.1 | 2130 |
| BF-4 | 4 | 1900×2000×1200 | 650 | 8 | 2--4 | 15/1.5 | 0.9-1.1 | 2585 |
| BF-6 | 6 | 2200×2350×1300 | 700 | 7.5 | 3--6 | 18.5/1.5 | 0.9-1.1 | 3300 |
| BF-8 | 8 | 2250×2850×1400 | 760 | 7.5 | 4--8 | 30/1.5 | 0.9-1.1 | 4130 |
| BF-10 | 10 | 2250×2850×1700 | 760 | 7.52 | 5--10 | 30/1.5 | 0.9-1.1 | 4660 |
| BF-16 | 16 | 2850×3800×1700 | 850 | 8.7 | 8--16 | 37/1.5 | 0.9-1.1 | 8320 |
| BF-20 | 20 | 2850×3800×2000 | 850 | 8.7 | 10--20 | 37/1.5 | 0.9-1.1 | 8670 |
| BF-24 | 24 | 3150×4150×2000 | 920 | 8.7 | 12--24 | 45/1.5 | 0.9-1.1 | 8970 |
| XJB棒型浮选机 Bar type flotation machine |  |  |  |  |  |  |  |  |
| XJB-10 | 1 | 1300×1300×680 | 400/410 | 转速400/410 | 1.5-1.7 | 5.5/4 |  | 1336 |
| XJB-10D | 1 | 1300×1300×680 | 400/410 | 400/410 | 1.5-1.7 | 5.5/4 |  | 1370 |
| XJB-20 | 2 | 1750×1750×700 | 450/540 | 360/360 | 1.5-4 | 15.0/11 |  | 2268 |
| XJB-20D | 2 | 1750×1750×700 | 450/540 | 360/360 | 1.5-4 | 15.0/11 |  | 2330 |
| XJB-40 | 4 |  | 700/510 | 280/280 | 2--4 | 18.5/18.5 |  |  |
| XJB-40D | 4 |  | 700/510 | 280/280 | 2--4 | 18.5/18.5 |  |  |

表7

| GF、XJQX型自吸气自吸浆机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating flotation machine with auto air suction |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-7 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机 功率 | 空气吸入量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| GF-0.35 | 0.35 | 700×700×730 |  |  | 0.1-0.2 | 1.5/0.75 | 1.2 | 470 |
| GF-0.7 | 0.7 | 900×900×900 |  |  | 0.1-0.4 | 3/1.1 | 1.2 | 932 |
| GF-1.1 | 1.1 | 1100×1100×1000 |  |  | 0.2-0.5 | 5/1.1 | 1.2 | 1370 |
| GF-2 | 2 | 1400×1400×1150 |  |  | 0.3-1.0 | 7.5/1.5 | 1.2 | 1750 |
| GF-3 | 3 | 1500×1850×1200 |  |  | 0.5-1.5 | 11/1.5 | 1.2 | 2230 |
| GF-4 | 4 | 1600×2150×1250 |  |  | 0.5-2 | 15/1.5 | 1.2 | 2585 |
| GF-6 | 6 | 2000×2500×1300 |  |  | 1-3 | 22/1.5 | 1.2 | 3300 |
| GF-8 | 8 | 2200×2900×1400 |  |  | 1-4 | 30/1.5 | 1.2 | 4130 |
| GF-10 | 10 | 2200×2900×1700 |  |  | 2-6 | 30/1.5 | 1.2 | 4500 |
| GF-16 | 16 | 2850×3800×1700 |  |  | 3-8 | 45/2.2 | 1.2 | 8320 |
| GF-20 | 20 | 2850×3800×2000 |  |  | 4-10 | 45/2.2 | 1.2 | 8670 |
| GF-24 | 24 | 3150×4150×2000 |  |  | 5-12 | 55/2.2 | 1.2 | 8970 |
| GF-28 | 28 | 3150×4150×2300 |  |  | 5-14 | 55/2.2 | 1.2 | 9480 |
| GF-42 | 42 | 3600×4800×2650 |  |  | 8-20 | 75/3 | 1.2 | 19400 |
| XJQX-40 | 4 |  | 400/500 | 315 | 3-5 | 15/1.1 | 1 | 4031 |
| XJQX-80 | 8 |  | 560/700 | 225 | 4-6 | 30/1.1 | 1 | 6057 |
| XJQX-100 | 10 |  | 540/700 | 233 | 4-10 | 30/1.5 | 1 | 7644 |
| XJQX-160 | 16 |  | 700/1000 | 180 | 5-16 | 55/1.5 | 1 | 10375 |
| XJQX-200 | 20 |  | 700/1000 | 180 | 5-20 | 55/1.5 | 1 | 10583 |

表8

| BS-K、KYF型充气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating aeration flotation machine |  |  |  |  |  |  |  |  |
| BS-K型浮选机属深槽型、充气型浮选机，叶轮只起搅拌矿浆、循环矿浆和分散空气的作用，因而易损件磨损较轻，其功率比其它类型浮选机较省。该机无自吸矿浆能力，需要阶梯配置，作业中间产品返回需用泡沫泵。 |  |  |  |  |  |  |  |  |
| Model-BS-K is a kind of deep tank lotation machine with aeration. Again, the impeller plays roles of agitating shurry, cycling slurry and distributing air. Therefore, the wearable parts suffer less waaring. It requires less power than the other models. This machine has no ability to pump slurry, thus bench arrangement is necessary, and foam pump is needed. |  |  |  |  |  |  |  |  |
| XCF型与KYF型浮选机均属充气型浮选机，叶轮直径小，圆周速度低，可降低功率30-50%；槽内设有一个空气分配器，因而空气分散均匀；叶轮起离心泵作用，可使固体颗粒充分悬浮；采用U型槽结构，可使尾砂沉积最少；叶轮结构及叶片间隙流道设计合理，叶轮磨损较均匀，叶轮、定子使用寿命长。KYF型无自吸矿浆能力，功率较低；XCF型具有自吸矿浆能力，可水平配置，不需要泡沫泵，但功耗较KYF略高一些，因而一般都将XCF型和高KYF型配置成机组，XCF型为吸入槽，KYF型为直流槽，联合机组可水平配置，不需泡沫泵。 |  |  |  |  |  |  |  |  |
| Models XCF and KYF are enforced aeration flotation machine. It has a smaller diameter of impeller, thus lower peripheral speed, saving 30%-50% of power. Because and air distributor is equipped in the tank, air is evenly dispersed. The impeller acts as a centrifugal pump, so as to make the solid particles suspending. The tank is made as Utype, reducing sand settlement to the least. Due to reasonable design of the impeller structure and the impeller space,impeller wearing is even, so, the service life of the impeller and stator are extended. Model KYF is unable to spontaneously suck slurry, while has low power consumption. In contrast, model XCF has the ability to automati-cally suck slurry, and may be allocated horizontally without need for foam pump, but consumes more nower than model KYF. Thereore, model XCF and model KYF are combined into a set, i.e., XCF as the sucking tank, and KYF as the direct tank. The combined set can be arranged horizontally without foam pump either. |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-8 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机 功率 | 最大充气量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Max.air flow | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| BS-K1 | 1 | 1000×1000×1100 | 350 | 281 | 0.2-1 | 3/1.1 | 0-2 | 998 |
| BS-K2 | 2 | 1500×1500×1300 | 420 | 260 | 0.5-3 | 5.5/1.1 | 2--3 | 1480 |
| BS-K3 | 3 | 1600×1600×1400 | 500 | 230 | 0.5-3 | 7.5/1.1 | 2--6 | 2001 |

表9

| BS-K、KYF型充气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating aeration flotation machine |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-9 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机 功率 | 最大充气量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Max.air flow | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| BS-K4 | 4 | 1850×1850×1550 | 500 | 225 | 0.5-4 | 7.5/1.1 | 3--6 | 2200 |
| BS-K6 | 6 | 2100×2100×1680 | 650 | 197 | 1--6 | 18.5/1.1 | 4--10 | 3278 |
| BS-K8 | 8 | 2250×2250×1700 | 650 | 190 | 1--8 | 15/1.1 | 4--10 | 4832 |
| BS-K16 | 16 | 2950×2720×2380 | 750 | 165 | 2--16 | 30/1.1 | 6--15 | 8131 |
| BS-K24 | 24 | 3200×3200×2800 | 830 | 159 | 7--24 | 37/1.1 | 8--18 | 9820 |
| BS-K30 | 30 | 3500×3500×3025 | 880 | 151 | 7---30 | 37/1.1 | 10--20 | 11100 |
| BS-K38 | 38 | 3600×3600×3400 | 910 | 141 | 10-38 | 45/1.1 | 10--20 | 13820 |
| KYF-1 | 1 | 1000×1000×1100 | 340 | 281 | 0.2-1 | 4/1.1 | 2 | 1056 |
| KYF-2 | 2 | 1300×1300×1250 | 410 | 247 | 0.4-2 | 5.5/1.1 | 2 | 1346 |
| KYF-3 | 3 | 1600×1600×1400 | 480 | 219 | 0.6-3 | 7.5/1.1 | 2 | 2074 |
| KYF-4 | 4 | 1800×1800×1500 | 550 | 200 | 1.2-4 | 11/1.5 | 2 | 2100 |
| KYF-6 | 6 | 2050×2050×1750 | 550 | 200 | 1.2-6 | 11/1.5 | 2 | 3278 |
| KYF-8 | 8 | 2200×2200×1950 | 630 | 175 | 3-8 | 15/1.5 | 2 | 3857 |
| KYF-10 | 10 | 2400×2400×2100 | 660 | 175 | 3-10 | 15/1.5 | 2 | 4334 |
| KYF-16 | 16 | 2800×2800×2400 | 740 | 160 | 4-16 | 30/1.5 | 2 | 7545 |
| KYF-20 | 20 | 3000×3000×2700 | 740 | 160 | 4-20 | 30/1.5 | 2 | 8240 |
| KYF-24 | 24 | 3100×3100×2900 | 800 | 150 | 4-24 | 30/1.5 | 2 | 9820 |
| KYF-30 | 30 | 3500×3500×3025 | 900 | 140 | 10-30 | 37/1.5 | 2 | 13820 |
| KYF-38 | 38 | 3600×3600×3400 | 880 | 138 | 10-38 | 45/1.5 | 1.8 | 16300 |
| KYF-40 | 40 | 3800×3800×3400 | 1050 | 138 | 8-40 | 45/1.5 | 1.8 | 17097 |
| KYF-50 | 50 | 4400×4400×3500 | 1030 | 131 | 10-40 | 75/1.5 | 1.5 | 22000 |
| KYF-70 | 70 | 5100×5100×3800 | 1120 | 121 | 13-50 | 90/1.5 | 1.5 | 26200 |
| KYF-100 | 100 | 5900×5900×4200 | 1260 |  | 20-60 | 110/1.5 | 1.5 | 36200 |

表10

| XCF、XCF/KYF型充气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating aeration flotation machine |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-10 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机 功率 | 最大充气量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Max.air flow | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| XCF-1 | 1 | 1000×1000×1100 | 400 | 358 | 0.2-1 | 5.5/1.1 | 2 | 920 |
| XCF-2 | 2 | 1300×1300×1250 | 460 | 331 | 0.4-2 | 7.5/1.1 | 2 | 1158 |
| XCF-3 | 3 | 1600×1600×1400 | 540 | 266 | 0.6-3 | 11/1.5 | 2 | 2172 |
| XCF-4 | 4 | 1800×1800×1500 | 620 | 215 | 1.2-4 | 15/1.5 | 2 | 2375 |
| XCF-6 | 6 | 2050×2050×1750 | 620 | 215 | 3--6 | 15/1.5 | 2 | 3545 |
| XCF-8 | 8 | 2200×2200×1950 | 720 | 185 | 3--8 | 22/1.5 | 2 | 4142 |
| XCF-10 | 10 | 2400×2400×2100 | 760 | 185 | 3--10 | 22/1.5 | 2 | 4894 |
| XCF-16 | 16 | 2800×2800×2400 | 860 | 160 | 4--16 | 37/1.5 | 2 | 6928 |
| XCF-20 | 20 | 3000×3000×2700 | 910 | 160 | 4--20 | 37/1.5 | 2 | 9200 |
| XCF-24 | 24 | 3100×3100×2900 | 950 | 153 | 4--24 | 37/1.5 | 2 | 10819 |
| XCF-30 | 30 | 3500×3500×3025 | 880 | 140 | 10--30 | 45/1.5 | 2 | 14810 |
| XCF-38 | 38 | 3600×3600×3400 | 1050 | 138 | 10-38 | 45/1.5 | 1.8 | 16900 |
| XCF-40 | 40 | 3800×3800×3400 | 1050 | 138 | 10-40 | 45/1.5 | 1.8 | 18790 |
| XCF-50 | 50 | 4400×4400×3500 | 1200 | 134 | 10-40 | 90/1.5 | 1.5 | 22000 |
| XCF-70 | 70 | 5100×5100×3800 | 1120 | 121 | 13-50 | 90/1.5 | 1.5 | 26200 |
| XCF-100 | 100 | 5900×5900×4200 | 1260 |  | 20-60 | 132/1.5 | 1.5 | 33500 |
| XCF/KYF型充气机械搅拌式浮选机组 |  |  |  |  |  |  |  |  |
| specification of mechanical agitating aeration flotation machine set |  |  |  |  |  |  |  |  |
| XCF/KYF-1 | 1 | 1000×1000×1100 | 400/340 | 358/281 | 0.2-1 | 5.5/4/1.1 | 2 | 920/1056 |
| XCF/KYF-2 | 2 | 1300×1300×1250 | 470/410 | 331/247 | 0.4-2 | 7.5/5.5/1.1 | 2 | 1158/1346 |
| XCF/KYF-3 | 3 | 1600×1600×1400 | 540/480 | 266/219 | 0.6-3 | 11/7.5/1.5 | 2 | 2172/2074 |
| XCF/KYF-4 | 4 | 1800×1800×1500 | 620/550 | 215/200 | 1.2-4 | 15/11/1.5 | 2 | 2375/2100 |
| XCF/KYF-6 | 6 | 2050×2050×1750 | 620/550 | 215/200 | 3--6 | 15/11/1.5 | 2 | 3545/3278 |
| XCF/KYF-8 | 8 | 2200×2200×1950 | 720/630 | 185/175 | 3--8 | 22/15/1.5 | 2 | 4142/3857 |
| XCF/KYF-10 | 10 | 2400×2400×2100 | 760/660 | 185/175 | 3--10 | 22/151.5 | 2 | 4894/4334 |

表11

| XCF/KYF、XCF/BSK型充气机械搅拌式浮选机组技术参数. specification of mechanical agitating aeration flotation machine set. №H-11. 型号规格Model; 容积; 槽体尺寸; 叶轮直径; 叶轮转速; 处理 能力; 电机功率; 最大 充气量; 单槽质量. Volume; cell size; Impeller Dia.; Impeller speed; capacity; power; Max.air flow; singe cell weight. m3; mm; mm; r/min; m3/min; kw; m3/m2min; kg. XCF/KYF-16; 16; 2800×2800×2400; 860/740; 160; 4--6; 37/30/1.5; 2; 6928/7575. XCF/KYF-20; 20; 3000×3000×2700; 910/780; 160; 4--20; 37/30/1.5; 2; 9200/8240. XCF/KYF-24; 24; 3100×3100×2900; 950/800; 153; 4--24; 37/30/1.5; 2; 10819/9820. XCF/KYF-30; 30; 3500×3500×3025; 880/900; 140; 10--30; 45/37/1.5; 2; 14810/13820. XCF/KYF-38; 38; 3600×360×3400; 1050/880; 138; 10--38; 45/45/1.5; 1.8; 16900/16300. XCF/KYF-40; 40; 3800×3800×3400; 1050/1050; 138; 10--40; 45/45/1.5; 1.8; 18790/17097. XCF/KYF-50; 50; 4400×4400×3500; 1200/1030; 134; 10--40; 90/75/1.5; 1.5; 22000/22000. XCF/KYF-70; 70; 5100×5100×3800; 1120/1120; 121; 13--50; 90/90/1.5; 1.5; 26200/26200. XCF/KYF-100; 100; 5900×5900×4200; 1260/1260; 20--60; 132/110/1.5; 1.5; 33500/26200. XCF/BSK型充气搅拌式浮选机组 sub-aeration machine set external blower. XCF/BSK-2; 2; 1300×1300×1250; 460/420; 331/260; 0.5-3; 7.5/5.5/1.1; 2--3; 1659/1480. XCF/BSK-4; 4; 1800×1800×1500; 620/500; 215/230; 0.5-4; 15/7.5/1.1; 3--6; 2669/2200. XCF/BSK-6; 6; 2050×2050×1750; 620/650; 215/197; 1--6; 15/18.5/1.1; 4--10; 3545/3278. XCF/BSK-8; 8; 2200×2200×1950; 720/650; 185/190; 1--8; 22/15/1.1; 4--10; 3868/4832. XCF/BSK-16; 16; 2800×2800×2400; 860/750; 160/170; 2--15; 37/30/1.1; 6--15; 6520/8131. XCF/BSK-24; 24; 3100×3100×2900; 950/830; 153/159; 7--20; 37/37/1.1; 8-18; 8000/9820. XCF/BSK-38; 38; 3600×3600×3400; 1050/910; 138/141; 10--30; 45/45/1.1; 10-20; 11000/13820. |  |
| --- | --- |

表12

| CHF-X、XHF、BSF型充气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specifications of flotation machine |  |  |  |  |  |  |  |  |
| XHF型浮选机有自吸矿浆能力,水平配置,不需泡沫泵,其叶轮直径大,主轴转速高.BSF型浮选机单独使用可形成阶梯布置的浮选统;与XHF浮选机联合使用可形成水平布置的浮选系统. |  |  |  |  |  |  |  |  |
| 两种浮选机都属深槽型浮选机,采用鼓风机供气。叶轮只起搅拌矿浆、循环矿浆和分散空气的作用。叶轮直径小，圆周速度底，叶轮与定子之间的间隙大，减轻了叶轮与定子的磨损。该机叶轮结构及叶片间隙流道设计合理，叶轮磨损较均匀，叶轮、定子使用寿命长。 |  |  |  |  |  |  |  |  |
| Model XHF is able to automaticall suck slurry ,and it may be allocated horizontally without foam pump.It has a big diameter of impeller ,and high turning speed of the main shaft.Model BSF can be separately used to make up a flotation system of bench style arrangement.When combined with XHF,it may consist a horizontal flotation system. |  |  |  |  |  |  |  |  |
| The above two are of deep tank flotation machine,fan being used for air supply.The impeller play roles of agitating slurry,cycling slurry ,cycling slurry and distributing air.Because of small diameter of impeller,low peripheral speed,and big space between the impeller and the stator,wearing of the impeller and the stator is reduced.This machine features sensible designs lf the impeller structure and the flow channel between the impellers.As a result,impeller wearing is even,and the impeller and the stator lasts loner. |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-12 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机 功率 | 最大充气量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Max.air flow | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| CHF-X3.5 | 3.5 | 1700×1700×1300 | 750 | 180 | 2-7 | 11 | 1.5-1.8 | 2100 |
| CHF-X7 | 7 | 2000×2000×1800 | 900 | 150 | 4-12 | 18.5 | 1.5-1.8 | 4100 |
| CHF-X14 | 14 | 2000×4000×1800 | 900 | 150 | 5-20 | 18.5 | 1.5-1.8 | 7900 |
| XHF-1 | 1 | 1000×1000×1100 | 400 | 385 | 0.2-1 | 5.5/1.1 | 2 | 1154 |
| XHF-2 | 2 | 1300×1300×1250 | 460 | 331 | 0.4-2 | 7.5/1.1 | 2 | 1659 |
| XHF-3 | 3 | 1600×1600×1400 | 540 | 266 | 0.6-3 | 11/1.5 | 2 | 2259 |
| XHF-4 | 4 | 1800×1800×1500 | 620 | 215 | 1.2-4 | 15/1.5 | 2 | 2669 |
| XHF-8 | 8 | 2200×2200×2100 | 720 | 185 | 3--8 | 22/1.5 | 2 | 3868 |
| XHF-16 | 16 | 2800×2800×2400 | 860 | 160 | 4-16 | 37/1.5 | 2 | 6520 |

表13

| CHF-X、XHF、BSF型充气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating aeration flotation machine |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-13 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理 能力 | 电机 功率 | 最大 充气量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Max.air flow | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| XHF-24 | 24 | 3100×3100×2900 | 950 | 153 | 4-24 | 37/1.5 | 2 | 8000 |
| XHF-38 | 38 | 3600×3600×3400 | 1050 | 138 | 10-38 | 45/1.5 | 2 | 11000 |
| BSF-2.2 | 2.2 | 1500×1500×1300 | 420 | 260 | 0.5-3 | 5.5/1.1 | 2--3 | 1750 |
| BSF-4 | 4 | 1850×1850×1550 | 500 | 230 | 0.5-4 | 7.5/1.1 | 3--6 | 2568 |
| BSF-6 | 6 | 2100×2100×1680 | 650 | 197 | 1- 6 | 18.5/1.1 | 4--10 | 3760 |
| BSF-8 | 8 | 2250×2250×1700 | 650 | 190 | 1-8 | 15/1.1 | 4---10 | 6463 |
| BSF-16 | 16 | 2950×2720×2380 | 750 | 170 | 2-15 | 30/1.1 | 6--15 | 9231 |
| BSF-24 | 24 | 3200×3200×2800 | 830 | 159 | 7-20 | 37/1.1 | 8--18 | 10600 |
| BSF-38 | 38 | 3600×3600×3400 | 910 | 141 | 10-30 | 45/1.1 | 10--20 | 12677 |

表14

| XJC、BS-X、CLF型充气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechanical agitating aeration flotation machine |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-14 |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机 功率 | 最大充气量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Max.air flow | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| XJC-40 | 4 | 1700×1700×1600 | 700 | 190 | 3--6 | 11/1.1 | 2-3.5 | 2739 |
| XJC-80 | 8 | 2200×2200×1800 | 900 | 170 | 4--8 | 22/1.1 | 6--8 | 3854 |
| XJC-160 | 16 | 2800×2800×2200 | 1000 | 160 | 8--20 | 30/1.1 | 6-9.5 | 6077 |
| BS-X4 | 4 | 1700×1700×1600 | 700 | 190 | 0.8-4 | 11/1.5 | 3-3.5 | 2150 |
| BS-X8 | 8 | 2200×2200×1800 | 900 | 170 | 2--8 | 22/1.5 | 6--7 | 4200 |
| CLF型粗颗粒浮选机技术参数 |  |  |  |  |  |  |  |  |
| specification of mechanical agitating aeration flotation maching |  |  |  |  |  |  |  |  |
| 型号规格Model | 容积 | 槽体尺寸 | 叶轮直径 | 叶轮转速 | 处理能力 | 电机 功率 | 最大充气量 | 单槽质量 |
|  | Volume | cell size | Impeller Dia. | Impeller speed | capacity | power | Max.air flow | singe cell weight |
|  | m3 | mm | mm | r/min | m3/min | kw | m3/m2min | kg |
| CLF-2 | 2 | 1200×1600×1250 |  |  | 0.5-2 | 7.5/5.5 | 0-5 | 1591/1418 |
| CLF-4 | 4 | 1600×2100×1500 | 580/620 | 220/231 | 1-4 | 15/11 | 0-7 | 3002/2702 |
| CLF-8 | 8 | 1900×2500×1950 |  |  | 1-6 | 22/15 | 0-12 | 5168/4654 |
| CLF-16 | 16 | 2500×3200×2400 |  |  | 1-8 | 45/37 | 0-16 | 9230/8970 |

表15

| XJM-S、XJX、XJZ、XJN型煤用充气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of mechaanical agitating aeration flotation machine for coal |  |  |  |  |  |  |  |  |
| XJM-S(2000)系列浮选机用于浮选-0.5mm粒级各种可浮性煤泥，也可用于浮选其他矿物，现已成为选煤用的主要浮选设备。由于具有独特的入料方式和搅拌机构，优化的流体动力学参数和高选择性分离设计，因此该系列浮选机具有以下特点：①独特的：“”入料方式——“假底底吸、周边串流”，矿浆流态合理，通过能力大，浮选速度快；②双层伞形叶轮设计，空气流道通畅，槽内呈“W型”矿浆流态，可有效降低功耗；③“单控点、双系统进气”，充气效能高，可调范围广（充气速度可调范围在0.5-1.2m3/m2.min),可实现充气量的‘在线'调控；④分体式定子设计，实现叶轮下吸口与吸浆管自然对中，安装精度得到保证；⑤“浸没式中矿箱”使矿化气泡与排出的矿浆逆向运动，可提高分离精度；⑥粗度级的浮选效果优于同规格其他类型的浮选机（柱），对细粒级的选择性高，可获得优质浮选产品，精煤回收率高；⑦能耗和药耗低，浮选机装机及实耗功率均小于国内外同类型同规格的其他浮选机；⑧优质耐磨材料，叶轮和定子使用寿命长；⑨占地面积小，运转可靠，操作维护方便，维护量小等优点。 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-15 |
| 型号规格 | 容积 | 槽数 | 叶轮直径 | 叶轮周速 | 处理能力 | 电机 功率 | 充气量 | 单槽质量 |
| Model | Volume |  | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | <个> | mm | r/min | m3/min | kw | m3/m2min | kg |
| XJM-S3 | 3 | 3-6 | 460 | 8.4 | 200 | 11/1.5 | 0.6-1.2 |  |
| XJM-S4 | 4 | 3-6 | 530 | 8.4 | 250 | 15/1.5 | 0.6-1.2 | 9684/3 |
| XJM-S6 | 6 | 3-6 | 600 | 8.4 | 300 | 18.5/1.5 | 0.6-1.2 |  |
| XJM-S8 | 8 | 3-6 | 700 | 8.4 | 400 | 22/1.5 | 0.6-1.2 | 15100/3 |
| XJM-S12 | 12 | 3-6 | 800 | 8.9 | 600 | 30/1.5 | 0.6-1.2 | 22863/3 |
| XJM-S14 | 14 | 3-6 | 800 | 8.9 | 680 | 30/1.5 | 0.6-1.2 |  |
| XJM-S16 | 16 | 3-6 | 860 | 8.9 | 750 | 37/1.5 | 0.6-1.2 | 27344/3 |
| XJM-S20 | 20 | 3-6 | 920 | 8.9 | 850 | 45/2.2 | 0.6-1.2 |  |
| XJM-4 | 4 | 6 | 530 | 8.4 | 200 | 15/1.1 | 0.6-1.2 | 10.49 |
| XJM-6 | 6 | 5 | 600 | 8.4 | 300 | 18.5/2.2 | 0.6-1.2 | 16.66 |
| XJM-8 | 8 | 4 | 660 | 8.6 | 400 | 22/2.2 | 0.6-1.2 | 18.62 |

表16

| XJZ型煤用充气机械搅拌式浮选机技术参数 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| specification of Mechanical agitating aeration flotation machine for coal |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | №H-16 |
| 型号规格Model | 容积 | 槽数 | 叶轮直径 | 叶轮周速 | 处理能力 | 电机 功率 | 充气量 | 单槽质量 |
|  | Volume |  | Impeller Dia. | Impeller speed | capacity | power | Air flow sucked | singe cell weight |
|  | m3 | 个 | mm | r/min | m3/min | kw | m3/m2min | kg |
| XJZ-6 | 6 | 4 |  | 9 | 300 | 22/1.5 | 0.6-1.2 | 15 |
| XJZ-8 | 8 | 5 | 660 | 9 | 400 | 30/1.5 | 0.6-1.2 | 22 |
| XJZ-12 | 12 | 5 | 760 | 8.8 | 500 | 37/2.2 | 0.6-1.2 | 31 |
| XJZ-13 | 13 | 4 | 660 | 6.6 | 600 | 22/2.2 | 0.6-1.2 | 24 |
| XJZ-14 | 14 | 5 | 660 | 6.6 | 700 | 30/0.75 | 0.6-1.2 | 32 |
| XJX-T8 | 8 | 4-6 | 660 | 8.6 | 400 | 30/1.94 | 0.6-1.2 | 25.96 |
| XJX-T12 | 12 | 4-5 | 760 | 8.8 | 700 | 37/1.94 | 0.6-1.2 | 35.7 |
| XJN-8 | 8 | 6 | 560 | 转速220 | 500 | 22 | 0.6-1.2 | 30 |
| XJN-14 | 14 | 6 | 660 | 190 | 680 | 30 | 0.6-1.2 | 40.3 |
| XJN-28 | 28 | 6 | 762 | 185 | 1600 | 55 | 0.6-1.2 | 65 |

表17

IF型煤用充气浮选机技术参数

Specification of mechaanical agitating aeration flotation machine for coal

№H-17

| 型号规格 | 容积 | 最大矿浆量 | 最大压气量 | 气压 | 控制气压 | 电机功率 power | 质量 weight |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Model | m3 | m3/h | Nm3/h | Mpa | Mpa | kw | kg |
| IF-30R | 36 | 1200 | <780 | 0.05 | 0.3-0.6 | 30 | 10400 |
| IF-57R | 60 | 2400 | <1200 | 0.05 | 0.3-0.6 | 55 | 16500 |
| IF-9S | 9.2 | 300 | <90 | 0.06 | 0.3-0.6 | 15 | 6200 |
| IF-19SR | 19 | 500 | <90 | 0.06 | 0.3 | 30 | 1100 |
| IF-20RC | 23.3 | 500 | <480 | 0.05 | 0.3-0.6 | 30 | 1100 |
| IF-30RC | 34 | 500 | <480 | 0.05 | 0.3-0.6 | 30 | 13100 |
| IF-45W | 45 | 780 | <1200 | 0.045 | 0.3-0.6 | 45 | 18600 |

FJC型煤用喷射式浮选机(四槽)技术参数
Specification of jet flotation machine for coal

| 型号规格 | 处理能力m3/h | 刮泡机构减速机 |  | 电动执行器 |  | 渣 浆 泵 |  |  |  | 外形尺寸mm | 质量kg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 型号 | 功率KW | 型号 | 行程mm | 型号 | 流量m3/h | 扬程Mpa | 功率KW |  |  |
| FJC4 | 100-160 | BWD3-43-2.2 | 2.2 | DKZ-510 | 0-100 | 150ZJD-A40 | ≥230 | ≥0.22 | 30 | 8316×2780×2150 | 10800 |
| FJC8 | 200-320 | BWD3-43-2.2 | 2.2 | DKZ-510 | 0-100 | 200ZJD-B45(41) | ≥460 | ≥0.22 | 45 | 9927×3600×2483 | 15900 |
| FJC12 | 290-480 | BWD3-43-2.2 | 2.2 | DKZ-510 | 0-100 | 200ZJD-B45(44) | ≥580 | ≥0.22 | 55 | 11785×3800×2820 | 24100 |
| FJC16 | 400-640 | BWD4-59-3 | 3.0 | DKZ-510 | 0-100 | 300ZJD-A60(55) | ≥800 | ≥0.22 | 75 | 12785×4070×3020 | 29400 |
| FJC20 | 600-800 | BWD4-59-3 | 3.0 | DKZ-510 | 0-100 | 300ZJD-A60(58) | ≥970 | ≥0.22 | 95 | 13835×4300×3120 | 34000 |

XPM型喷射型浮选机技术参数
Specification of jet flotation machine for coal

| 型号规格 | 容积m3 | 槽数（个） | 产量m3/h | 功率kw | 单槽质量kg |
| --- | --- | --- | --- | --- | --- |
| XPM-1.5 | 1.5 | 4 | 7-13.5 |  | 660 |
| XPM-4 | 4 | 6 | 19-36 | 55/1.94 | 2100 |
| XPM-6 | 6 | 6 | 28-54 |  |  |
| XPM-8 | 8 | 6 | 38-72 | 75/1.94 | 2633 |

表18

| FCSMC、FXZ浮选柱技术参数 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| specifications of Floatobast |  |  |  |  |  |  |
| 工作原理：旋流微泡浮选柱采用射流原理，将旋流器与浮选柱有效结合。通过渣浆泵产生高压矿浆经气泡发生器(矿浆预备器）产生微泡，由旋流器后脱粗后<0.5mm矿物流入浮选柱进行选别。机器适用<0.5mm以下的煤泥、赤铁矿、有色矿、非金属矿、含油污水处理、废纸脱墨等细粒度、灰分高、泥质多的物料分选。具有节能高效，富集比大,泡沫产品品位高，工艺流程简化。节省设备投资25%、省电70%、节能药剂10%。占地少，结构简单，无传动部件，操作方便，易于自动化控制，维修方便等特点。 |  |  |  |  |  |  |
|  |  |  |  |  |  | №h-18 |
| 型号规格 Madel | 直径 Diameter m | 矿浆量 Pulp Throughput m3/h | 干量 Dry slurryt/h | 功率 Power KW | 质量 Weight t | 适用范围 Major pourpose 10000t/a |
| FXZ1000 | 1 | 50-60 | 4-5 | 13 |  | 10-15万t/年(煤) |
| FXZ1500 | 1.5 | 70-110 | 5-8 | 17 |  | 15-20万t/年(煤) |
| FXZ2000 | 2 | 110-180 | 8-12 | 30 |  | 20-30万t/年(煤) |
| FXZ3000 | 3 | 250-500 | 15-24 | 55 |  | 30-60万t/年(煤) |
| FCSMC1500 | 1.5 | 50-60 | 4-5 | 20 | 8 | 15-20万t/年(煤) |
| FCSMC2000 | 2 | 100-120 | 8-12 | 30 | 16 | 20-30万t/年(煤) |
| FCSMC3000 | 3 | 200-250 | 15-20 | 55 | 24 | 30-60万t/年(煤) |

anran5157收集整理

二〇〇八年七月二十四日